## Slide 1: Assessing the shelf life of spruce beetle-killed wood OMINECA SPRUCE BEETLE AND SHELF LIFE UPDATE Sorin Pasca, Director Applied Research and Innovation - CNC Jeanne Robert, Regional Entomologist - FLNRORD June 18, 2020

## Slide 2
Trees distribution with time since death

## Slide 3
Moisture content

## Slide 4
Presence of Checking
Chart: Estimated Time Since Death
| Live | 1 | 3 | 5 | 5+
Checks and cracks | 21 | 40 | 41 | 67 | 72
No checks and cracks | 79 | 60 | 59 | 33 | 28
Proportion of sample inventory with checking and cracking, across estimated TSD categories.

## Slide 5
Severity of Checking
Chart: Estimated Time Since Death
| Live | 1 | 3 | 5 | 5+
 | 0.027769 | 0.075961 | 0.089328 | 0.34887 | 0.46197
Checking length (depth) in samples, across estimated TSD categories. Lengths of checks and cracks were summed, doubled to account for the complete disc, and expressed as a proportion of sample disc diameter.

## Slide 6
Presence of Decay
Chart: Estimated Time Since Death
| Live | 1 | 3 | 5 | 5+
Decay | 29 | 46 | 54 | 69 | 62
No decay | 71 | 54 | 46 | 31 | 38
Proportion of sample inventory with observable decay across estimated TSD categories.

## Slide 7
Severity of Decay
Chart: Estimated Time Since Death
| Live | 1 | 3 | 5 | 5+
Percentage of decay of total area | 0.052379 | 0.065917 | 0.07525 | 0.097444 | 0.20714
Percentage sample area having decay and degradation, across estimated TSD categories.

## Slide 8
Many thanks to our sponsors and partners